## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Lectures and Working Class
Lectures & problem session on
Tuesday 10:00 : 11:30
Thursday 12:00 : 13:30
Problem sessions on Thursday alternating with lectures
Problem session teacher:
Dr. Matteo Montagnese, II P.I. room 318 m.montagnese@ph2.uni-koeln.de
Hand in problem sets on Tuesday’s (room 318).

## Slide 3: Literature
Introduction to Solid State Physics, Charles Kittel
Solid State Physics, Ibach & Lüth
Solid State Physics, Ashcroft & Mermin
Quantum theory of solids, Kittel
Principles of condensed matter physics, Chaikin & Lubensky
Many, many more

## Slide 4: States of matter
Liquid crystals
glasses
Amorphous solids
quasi crystals
nearly periodic crystals
PERIODIC CRYSTALS
Plasma
Gas
Liquid
SOLIDS

## Slide 5
Structure and symmetry
Binding
Diffraction -> reciprocal space
Vibrations & thermal properties, density of states
Electrons, Fermi Gas, Energy bands, semiconductors
Collective excitations (plasmons, excitons, etc.)
Dielectrical properties
Spins: magnetism & magnetic excitations

## Slide 6: II. Physikalisches Institut

## Slide 7: STRUCTURE
Kittel Ch.1

## Slide 8
Graphite
Silicon
Quartz
Protein
Quasi-crystal
Cu2O

## Slide 9: Structure
460 BC Demokritus: idea that matter is made of ‘atoms’
1611 J. Keppler: Snow Xtals made of spherical water molecules
1784 R.J. Haüy: Law of integral indices
1802 J. Dalton: atomic theory

## Slide 10: Structure
1784 R.J. Haüy: Law of integral indices
1850 A. Bravais: Space lattices
1895 W. Röntgen: X-rays (1st Nobel prize 1901, Work on cathode rays: Lenard 1905)
1912 M. van Laue: Diffraction (Nobel prize 1914)

## Slide 11
Si (FCC) 111 axis
Using hard X-rays (λ ~ a ~ 10 Å)

## Slide 12: Structure
1913/14 W.&L. Bragg: Diffraction (Nobel prize 1915)
1984 D. Shechtman: Quasicrystals (Chem. Nobel prize 2011)

## Slide 13: Symmetry
Translation symmetry:
vectors representing translations which
transform a structure into itself
Rotation symmetry:
Operations (rotations, mirrors) which
transform a structure into itself

## Slide 14
2л/6 rotation
Translations

## Slide 15: Lattice
Periodic Arrays of points
or
Lattice = set of fundamental translation vectors:
a1
a2
a1
a2
T = u1a1 + u2a2 + u3a3

## Slide 16: Crystal structure
Basis = group of atoms forming the unit cell:
Basis
Crystal Structure
Lattice + Basis = Crystal structure
Lattice

## Slide 17: Primitive cell
Minimal volume unit cell
Primitive cell
“Conventional” unit cell
A unit cell is not necessarily primitive!

## Slide 18: Primitive cell
Minimal volume unit cell
Primitive Translation vectors: a1 , a2 , a3
Primitive Lattice Cell = parallelepiped of a1 , a2 , a3
Many equivalent options to choose from,
Volume of Primitive Lattice cell: V = a1 . (a2 x a3 )
Wigner-Seitz Cell: Most symmetric choice of Primitive Cell

## Slide 19: Wigner-Seitz cell

## Slide 20: Symmetry elements
Translations: T = u1a1 + u2a2 + u3a3
Point group operations: Rotations and Mirrors
Combinations: Glide planes and Screw axes
6 fold rotation
Glide plane

## Slide 21: Two dimensional lattices (Net)
b
a1
a2
Ratio |a1/a2|
Angle b

## Slide 22: Two dimensional lattices (Net)

## Slide 23: 2D lattice types
1-fold + mirror:
Centered rectangular
2-fold: Rectangular
4-fold: Square
6-fold: Hexagonal
1-fold: Oblique
a1  a2; b
a1  a2; a = 90o
a1  a2; b = 90o
a1 = a2; b = 90o
a1 = a2; b = 120o

## Slide 24: 3D lattice types
Triclinic | 1 | No symmetries
Monoclinic | 2 | Two right angles
Orthorhombic | 4 | Three right angles
Tetragonal | 2 | Three right angles + 4 fold
Cubic (SC, FCC, BCC) | 3 | Three right angles + 4 fold + 3 fold
Trigonal | 1 | Three equal angles (not 90o)+ 3 fold
Hexagonal | 1 | Two right, one 120o + 6 fold
The 3D lattice types (14)

## Slide 25: Cubic lattices
Simple cubic
SC
Body centered
BCC
Na, K, Rb, Cs,
Fe, V, Cr, Mo, W
Face centered
FCC
Ni, Cu, Ag, Au, Pt,
Ne, Ar, Kr, Xe, Rn
Po

## Slide 26: NaCl Structure
Rocksalt structure
NaCl
SnTe
NaF
MgO

## Slide 27: Diamond structure
C,Si,Ge

## Slide 28: Hexagonal closed packed
H, He, N
Be, Mg
Co, Zn, Sc, Ti
Y, Zr, Tc, Ru, Cd
Hf, Re, Os, Tl,
Pr, Gd, Tb, Dy, Ho, Er, Lu

## Slide 29: Perovskite structure
Matthias Opel 2012 J. Phys. D: Appl. Phys. 45 033001
CaTiO3

## Slide 30: Planes and directions
Miller indices:
Find intercepts with axes of unit cell (in cell units).
Take reciprocals
Find (smallest) integers with the same ratio
x
y
z
O
() Planes
{} Equivalent planes Cubic
{100}: (100),(200),(001)
[] directions:
x-direction [100]

## Slide 31: Planes and directions
Miller indices:
Find intercepts with axes of unit cell (in cell units).
Take reciprocals
Find (smallest) integers with the same ratio
Intersections at (1,,)
Miller indices (100)
x
y
z
O

## Slide 32: Planes and directions
Miller indices:
Find intercepts with axes of unit cell (in cell units).
Take reciprocals
Find (smallest) integers with the same ratio
Intersections at (1,1,)
Miller indices (110)
x
y
z
O

## Slide 33: Planes and directions
Miller indices:
Find intercepts with axes of unit cell (in cell units).
Take reciprocals
Find (smallest) integers with the same ratio
Intersections at (1,1,1)
Miller indices (111)
x
y
z
O