## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Previously
Semiconductors:
Quantum Hall effect

## Slide 3: Today
Introduction magnetism

## Slide 4: MAGNETISM

## Slide 5: Water shows magnetism
Movies: High magnetic field laboratory Nijmegen

## Slide 6: Strawberries do it

## Slide 7: Even frogs

## Slide 9: ‘Classical’ Langevin diamagnetism
e- in B-field => Larmor precession with
Current of Z electrons per atom
Magnetic moment
Susceptibility of n atoms/volume
B
r
Force:
Notes: Rho is size orbit; r is projection perpendicular to B

## Slide 10: Magnetism
Diamagnetism:
- No magnetic moments
- No magnetic interaction - Water
- Response due to induced currents - Ideal gases
- Magnetization opposite to field - Superconductors
Paramagnetism:
- Magnetic moments (spin, orbit)
- Weak magnetic interactions - Metals
- Response due to orientation - ‘odd electron’ systems
- Magnetization in field direction - O2, biradicals
Ordered magnetism:
- Magnetic moments
- Strong magnetic interactions
- Response due to polarization - Fe, Ni, Co
- Ferro-, antiferro-, ferrimagnetic - Cr, high-Tc (CuO systems)

## Slide 11: Magnetization and susceptibility
Magnetic susceptibility:
Magnetization at T=0:
at finite T:
Only ground state (low T):

## Slide 12: Dia- & paramagnetism
H
M
T
c
H
M
1/T
c
Diamagnetism
Temperature independent
Paramagnetism
1/T dependence
M=cH

## Slide 13: QM treatment: orbit
Inclusion of the field in the motion:
Uniform H-field:
Gauge:
(app. G)
Notes: Vec. Identity A.(BxC)=B.(CxA)=C.(AxB)
Bohr magneton: mu = hbar e/2mc

## Slide 14: QM treatment: spin
Inclusion spin moment:
Curie
Van vleck
Langevin

## Slide 15
Everything is (dia)magnetic
Langevin diamagnetism: ‘shielding’ effect (Lenz law)
Meissner effect in superconductors c = -1
QM: inclusion of field Orbit Spin

## Slide 16: Magnetism
Diamagnetism:
- No magnetic moments
- No magnetic interaction
- Response due to induced currents - Ideal gases
- Magnetization opposite to field - Superconductors
Paramagnetism:
- Magnetic moments (spin, orbit)
- Weak magnetic interactions - Metals
- Response due to orientation - ‘odd electron’ systems
- Magnetization in field direction - O2, biradicals
Ordered magnetism:
- Magnetic moments
- Strong magnetic interactions
- Response due to polarization - Fe, Ni, Co
- Ferro-, antiferro-, ferrimagnetic - Cr, high-Tc (CuO systems)

## Slide 17: Para/diamagnetism
Curie
van Vleck
Langevin
diamagnetism

## Slide 18: Langevin diamagnetism
Low temperature, filled shell ions ( )
( SI: )

## Slide 19: Paramagnetism
alignment of weakly interacting magnetic moments in a magnetic field
Curie law c = q/T
Magnetic moments = spin, orbit
Ground state splitting (Curie)
Low lying excited states (van Vleck)
Density of states effects (Pauli magnetism)
First: Coupling between L and S: Russel-Saunders
H
M
T
c
1/T
c