## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Previously
Intro magnetism
- Diamagnetism: induced moments, no interaction
- Paramagnetism: needs moments, no interaction
- Ordered magnetism: needs moments & interaction

## Slide 3: Magnetism
Diamagnetism:
- No magnetic moments
- No magnetic interaction - Water
- Response due to induced currents - Ideal gases
- Magnetization opposite to field - Superconductors
Paramagnetism:
- Magnetic moments (spin, orbit)
- Weak magnetic interactions - Metals
- Response due to orientation - ‘odd electron’ systems
- Magnetization in field direction - O2, biradicals
Ordered magnetism:
- Magnetic moments
- Strong magnetic interactions
- Response due to polarization - Fe, Ni, Co
- Ferro-, antiferro-, ferrimagnetic - Cr, high-Tc (CuO systems)

## Slide 4: Today
Non-ordered magnetism
Magnetic moments
Crystal field effects

## Slide 5: Magnetization and susceptibility
Magnetic susceptibility:
Magnetization at T=0:
at finite T:
Only ground state (low T):

## Slide 6: Dia- & paramagnetism
H
M
T
c
H
M
1/T
c
Diamagnetism
Temperature independent
Paramagnetism
1/T dependence
M=cH

## Slide 7: QM treatment: orbit
Inclusion of the field in the motion:
Uniform H-field:
Gauge:
H//z
Notes: Vec. Identity A.(BxC)=B.(CxA)=C.(AxB)
Bohr magneton: mu = hbar e/2mc

## Slide 8: QM treatment: spin
Inclusion spin moment:
Curie
Van vleck
Langevin

## Slide 9
Everything is (dia)magnetic
Langevin diamagnetism: ‘shielding’ effect (Lenz law)
Meissner effect in superconductors c = -1
QM: inclusion of field Orbit Spin

## Slide 10: Magnetism
Diamagnetism:
- No magnetic moments
- No magnetic interaction
- Response due to induced currents - Ideal gases
- Magnetization opposite to field - Superconductors
Paramagnetism:
- Magnetic moments (spin, orbit)
- Weak magnetic interactions - Metals
- Response due to orientation - ‘odd electron’ systems
- Magnetization in field direction - O2, biradicals
Ordered magnetism:
- Magnetic moments
- Strong magnetic interactions
- Response due to polarization - Fe, Ni, Co
- Ferro-, antiferro-, ferrimagnetic - Cr, high-Tc (CuO systems)

## Slide 11: Langevin diamagnetism
Low temperature, filled shell ions ( )
( SI: )

## Slide 12: Paramagnetism
alignment of weakly interacting magnetic moments in a magnetic field
Curie law c = q/T
Magnetic moments = spin, orbit
Ground state splitting (Curie)
Low lying excited states (van Vleck)
Density of states effects (Pauli magnetism)
First: Coupling between L and S: Russel-Saunders
H
M
T
c
1/T
c

## Slide 13: Spin-Orbit interaction (qualitative)
Magnetic moment electron spin:
Current of the electron in orbit:
v
Energy of the spin in the field of the orbit:

## Slide 14: Partially filled shells
Lowest state has highest S
Lowest state has highest L( )
Lowest state has minimized LS interaction L+S for more than half filled (L,S opposite) |L-S| for less than half filled (L,S parallel)
Russel-Saunders coupling L,S and J commute with Hamiltonian. Quantum numbers L,Lz, S,Sz,J,Jz describe electronic state
Hund’s rules for n electrons in states
(Maximization anti-symmetry + Pauli)
States are characterized by

## Slide 15: Hund’s rules
d-shell ( ), 4 electrons
Mn3+,Cr2+
-2
-1
0
1
2
S=2
L=2 => 5D0
J=0
d-shell ( ), 5 electrons
Fe3+,Mn2+
d-shell ( ), 6 electrons
Fe2+
-2
-1
0
1
2
S=5/2
L=0 => 6S5/2
J=5/2
-2
-1
0
1
2
S=2
L=2 => 5D4
J=4
L = 0 1 2 3 4 5 6
X = S P D F G H I
Spectroscopic notation
2S+1XJ

## Slide 16: Rare earth elements
4f
6s2, 5d1
Rare earth elements:
Ce-Lu

## Slide 17: Rare earth elements
f-shell ( ), 7 electrons
Gd3+
S=7/2
L=0 => 8S7/2
J=7/2
-3
-2
-1
0
1
2
3
EF
La
4f
EF
Lu
4f
DOS
Energy

## Slide 18: Spectroscopic splitting factor Level splitting in a field

## Slide 19: Spectroscopic splitting
s shell, 1 electron:
2S1/2 (S=1/2,L=0,J=1/2) => gj=go=2
mBH
H
E
Mercury 3S1 – 3P0 transition (6s17s1 – 6s16p1, G.S. 6s25d10)
3S1
3P0
mJ=1
mJ=-1
mJ=0
gJ=2
gJ=0
mJ=0

## Slide 20
Experimental spectrum of the 4046.6 Å, 7 3S1 --> 6 3P0 transitions of atomic Hg with
(a) zero magnetic field
(b) a magnetic field B = 29.0 kG.
3S1
3P0
1
-1
0

## Slide 21: Crystal field splitting
Rare earth’s: 4f shell’s small (‘inner’ electrons)
Iron group: 3d shell’s on the outside
=> decoupling of L and S, J no longer good QN
=> splitting of the 2L+1 orbital states
=> Quenching of the orbital angular momentum (Lz0)

## Slide 22: 2D p states in a 2 fold potential
p-states in 2D:

## Slide 23
2Q

## Slide 24: With LS coupling

## Slide 25
-3.5
-3
-2.5
-2
-1.5
-1
-0.5
0
0.5
1
1.5
2
0
0.5
1
1.5
2
2.5
3
E/Q
l/Q

## Slide 26: Angular momentum
-0.6
-0.4
-0.2
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
0
0.5
1
1.5
2
2.5
3
3.5
4
J
l/Q
3/2
-1/2

## Slide 27: Magnetic moment
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
0
0.5
1
1.5
2
2.5
3
3.5
4
l/Q
2
0
m/ m B