## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Last time
Langevin diamagnetism
Moments
- Free ions
- LS couping
- Hund’s rules
- Spectroscopic splitting factor
- Crystal field effects

## Slide 3: Today
Paramagnetism
- Curie paramagnetism
- van Vleck magnetism
- Pauli paramagnetism

## Slide 4: PARAMAGNETISM

## Slide 5: Non-ordering magnetism
Langevin
(dia)
van Vleck
(para)
Curie
(para)
Spin-orbit coupling
Russel-Saunders, Hund’s rules
Crystal field splitting
Orbital magnetism
Spin magnetism

## Slide 6: Crystal field + spin-orbit
-1/2
0
1/2
1
3/2
0
1
2
3
4
J
l/Q
-4
-2
0
2
0
1
2
3
4
l/Q
E/Q
0
1/2
1
3/2
2
0
1
2
3
4
m/m B
l/Q

## Slide 7: Paramagnetism
“Alignment” of weakly interacting magnetic moments
Magnetic moments = spin, orbit
Ground state splitting (Curie)
Curie law c = C/T
Low lying excited states (van Vleck)
Metals: Density of states effects (Pauli magnetism)
H
M
T
c
1/T
c

## Slide 8: Curie law: G.S.
Ground state splitting:
L=0; S=1/2
Eg
H
Magnetic ground state

## Slide 9: Curie law: J=1/2
For J=1/2:
2
1
Thermal occupation Ni/N of the two states:
Magnetization M:

## Slide 10: Curie Law: J
More general: for G.S. with J: 2J+1 equi-spaced levels
With Brillouin function BJ:

## Slide 11: Curie Law: kT>>mBH
C: Curie constant
p: effective magneton number

## Slide 12: (C4H12N2)2Mn2Ga5(H2O)(PO4)8

## Slide 13: Curie law & Xtal field
Rare earth’s: 4f shell’s small (‘inner’ electrons)
=> p experimental  p calculated
except for Eu3+ and Sm3+
where low lying states mix in
Iron group: 3d shell’s on the outside
=> Crystal field important
p experimental  p calculated
as if Lz=0 (quenching)

## Slide 14: Effective magneton numbers
Transition metals
Lanthanides
0
2
4
6
8
10
0
2
4
6
8
10
12
Effective magneton number p
d-shell filling
P(J)
P(J=S)
0
2
4
6
8
10
12
14
0
2
4
6
8
10
12
Effective magneton number p
f-shell filling
P(J)
Ce3+
Lu3+
Sm3+
Ti3+
Fe3+
Cu2+
Eu3+
Sm3+

## Slide 15: van Vleck paramagnetism
Non-magnetic groundstate
Only one excited state D above GS,
kT<< D
Competition between
van Vleck and
Langevin
kT>> D:
Notes: kT>>Delta: ratio #ground/#excited ~ Delta/2kT => chi_vanvleck~ (Delta/2kT) * 2n<gmu<elem>>^2/Delta =n <gmu<elem>>^2 / kT

## Slide 16: Conduction electrons: Pauli paramagnetism
No field:
DOS
E
EF

## Slide 17: Pauli paramagnetism
:
DOS
E
EF
Landau (dia):
Pauli:

## Slide 18: Overview para/diamagnetism
Langevin (or Larmor)
diamagnetism
Superconductors, No moment systems
Pauli + Landau
Conduction electrons
van Vleck
Excited states
Curie C/T
Magnetic ground state
c
T

## Slide 19: Magnetism
Diamagnetism:
- No magnetic moments
- No magnetic interaction
- Response due to induced currents - Ideal gases
- Magnetization opposite to field - Superconductors
Paramagnetism:
- Magnetic moments (spin, orbit)
- Weak magnetic interactions - Metals
- Response due to orientation - ‘odd electron’ systems
- Magnetization in field direction - O2, biradicals
Ordered magnetism:
- Magnetic moments
- Strong magnetic interactions
- Response due to polarization - Fe, Ni, Co, Gd, Dy
- Ferro-, antiferro-, ferrimagnetic - CoO, FeO,
high-Tc (CuO systems)

## Slide 20: Ordered Magnetism
What if there is a strong interaction between moments ?
Ferromagnetism
Antiferromagnetism
Ferrimagnetism

## Slide 21: Ferromagnetic order
Mean field approximation:
Each moment experiences an additional
“field” proportional to the magnetization
due to the presence of all other moments.
M
T
Tc
Msat
Ordered
Para

## Slide 22: Mean field approach
T > Tc : No ordering, paramagnetic
c
T
Tc
More precise
Curie-Weiss
Law

## Slide 23: Mean field approach
T < Tc : Ordering, spontaneous ferromagnetic moment
For S=1/2 (Brouillin function, neglect external field):

## Slide 24: Spontaneous magnetization
m 
m
t=0.5
t=1
t=2
m=tanh(m/t)
M(T)/M(0) 
T/Tc 
1
1
S=2
S=5/2
S=1

## Slide 25
V. da Rocha Caffarena, T. Ogasawara, Mat. Res. 2003
Sm(3-x)HoxFe5O12 (x=2.4)