## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Last time
Paramagnetism
- Curie paramagnetism
- van Vleck magnetism
- Pauli paramagnetism
Ordered magnetism
- Curie-Weiss law
- Spontaneous magnetization
- Mean field approach

## Slide 3: Magnetization in Ni
Variation of saturation magnetisation with temperature for Nickel. (Data from Weiss and Forrer, 1926)
Variation of susceptibility with temperature for Nickel (Sucksmith and Pearce, 1938)

## Slide 4: Magnetic interaction
Iron: Tc ~ 1000 K

## Slide 5: Dipole-dipole interaction
In real materials: Tc ~ 102 – 103 K !!
 Dipole-dipole interaction hardly ever dominates
Dipole-dipole interaction is an anisotropic interaction

## Slide 6: Magnetic parameters
 | z | n [1022 cm-3] | g | p | C [K] | Tc [K] | J [meV] | l
Fe | 8 | 8.5 | 2 | 5.4 | 0.51 | 1043 | 2.3 | 2045
Co | 12 | 9 | 2 | 4.8 | 0.43 | 1388 | 2.3 | 3228
Ni | 12 | 9.1 | 2 | 3.2 | 0.19 | 627 | 0.6 | 3300
Gd | 12 | 3 | 2 | 8.0 | 0.40 | 293 | 0.2 | 733
 | M(0) [gauss] | M(0)/NmB | Hmf [106 gauss]
Fe | 1740 | 2.22 | 3.6
Co | 1446 | 1.72 | 4.7
Ni | 510 | 0.606 | 1.7
Gd | 2060 | 7.63 | 1.5
spin-orbit
canted, ferri
conduction electrons

## Slide 7: Interactions
Dipole – Dipole
Direct exchange (H2 molecule)
Indirect exchange
Double exchange
Anisotropic exchange
Rudeman Kittel Kasuya Yoshida (RKKY)
Stoner (“spontaneous Pauli”)

## Slide 8: H2 molecule
LCAO gives wrong solution (e.g. triplet ground state)
Correlated picture (Heitler-London approach) is better
  Starting point: two electron orbitals
  Wavefunctions (anti-symmetric under particle exchange)
  Spin parts:

## Slide 9: H2 molecule
Singlet ground state
Exchange energy: Pauli + Coulomb

## Slide 10: Exchange interaction
Heisenberg Hamiltonian
J>0: Ferro
J<0: Antiferro

## Slide 11: Direct exchange
Need direct wave function overlap
  Ferromagnetic
  Small in 4f, 5f elements
  Can be important in 3d oxides (but see indirect!)
  In 3d metals: electron delocalization
    Relatively small (but remember TiOX)
    Depends on orbital occupation and geometry
Oxide: ferro
‘hopping’: ferro
‘hopping’: antiferro

## Slide 12: Indirect exchange
Ground state antiferro
‘2*hopping’
Hopping 
delocalization 
energy gain
Energy: 2 hops = 2t; cost=U
 J ~ -t2/U
Examples: High Tc’s; MnO; MnF2
Pauli forbidden
Ground state antiferro
‘2*hopping’
Pauli forbidden
Ground state antiferro
‘2*hopping’

## Slide 13: Indirect exchange
Hopping  delocalization  energy gain
Energy: 2 hops = 2t; cost=U
 J ~ -t2/U
Examples: High Tc’s; MnO; MnF2; telephone number compound
Relatively strong (depends on U)
Usually AF (F when not same 3d, e.g.d3-d5)
Strongly dependent on angle of bonding
at 1800 strongly AF
at zero weakly F
(goodenough kanamouri rules
-J
angle
90
180

## Slide 14: (Sr,La,Ca)14Cu24O41
Eccleston et al., PRL 81, 1702 (1998)
J1=130 meV
J2= 70 meV
Δ=32 meV
J2
J1

## Slide 15: La9Ca5Cu24O41
c
a
T = Troom
μm
OCMP 2008