## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Last time
Heitler-London
Pauli + Coulomb
Exchange interactions

## Slide 3: Interactions
Dipole – Dipole
Direct exchange (H2 molecule)
Indirect exchange
Double exchange
Anisotropic exchange
Rudeman Kittel Kasuya Yoshida (RKKY)
Stoner (“spontaneous Pauli”)

## Slide 4: Exchange interaction
Heisenberg Hamiltonian
J>0: Ferro
J<0: Antiferro

## Slide 5: Direct exchange
Need direct wave function overlap
  Ferromagnetic
  Small in 4f, 5f elements
  Can be important in 3d oxides (but see indirect!)
  In 3d metals: electron delocalization
    Relatively small (but remember TiOX)
    Depends on orbital occupation and geometry
Oxide: ferro
‘hopping’: ferro
‘hopping’: antiferro

## Slide 6: Indirect exchange
Ground state antiferro
‘2*hopping’
Hopping 
delocalization 
energy gain
Energy: 2 hops = 2t; cost=U
 J ~ -t2/U
Examples: High Tc’s; MnO; MnF2
Pauli forbidden
Ground state antiferro
‘2*hopping’
Pauli forbidden
Ground state antiferro
‘2*hopping’

## Slide 7: Indirect exchange
Hopping  delocalization  energy gain
Energy: 2 hops = 2t; cost=U
 J ~ -t2/U
Examples: High Tc’s; MnO; MnF2; telephone number compound
Relatively strong (depends on U)
Usually AF (F when not same 3d, e.g.d3-d5)
Strongly dependent on angle of bonding
at 1800 strongly AF
at zero weakly F
(goodenough kanamouri rules
-J
angle
90
180

## Slide 8: (Sr,La,Ca)14Cu24O41
Eccleston et al., PRL 81, 1702 (1998)
J1=130 meV
J2= 70 meV
Δ=32 meV
J2
J1

## Slide 9: La9Ca5Cu24O41
c
a
T = Troom
μm
OCMP 2008

## Slide 10: Double exchange
Mixed valency
Usually ferro metal
Relatively strong
La1-xSrxMnO3 (Mn3+/Mn4+) Fe3O4 (AB2O4, Fe2+/Fe3+)
Mn3+
Mn4+
CMR in para phase close to Tcurie

## Slide 11: Anisotropic exchange
Dzyaloshinsky-Moriya interaction
Mixing in of excited d-states
LS coupling in excited state
If spins inversion symm. related then 0
From different from Heisenberg:
Favors perpendicular alignment
Examples: α-Fe2O3, MnCO3
In AF’s leads to net moment  weak ferro

## Slide 12: Multiferroics
Mostovoy & Cheong

## Slide 13: Magnetism in metals
No field:
DOS
E
EF
Free electron gas
Pauli paramagnetism, Landau diamagnetism
Curie-like (EF~kT)
Spontaneous spin polarization (Stoner)
RKKY

## Slide 14: Pauli paramagnetism
:
DOS
E
EF
Landau (dia):
Pauli:

## Slide 15: Stoner magnetism
Spontaneous spin polarization
DOS
E
} δE
2
2

## Slide 16: Stoner criterium
Exchange interaction
Density of States at EF
Product
Stoner criterium
In agreement with
Fe, Ni, Co ferromagnets

## Slide 17: Stoner magnetism
If UD(EF)<1 then still change in susceptibility

## Slide 18: Conduction electrons
4s-band
DOS
Energy
3d-band
EF
9.46 e-
0.54 e-
EF
5 e-
4.46 e-
0.54 e-
Net magnetization
due to d-band:
Ni 3d84s2

## Slide 19: Conduction electrons
4s-band
DOS
Energy
3d-band
EF
10 e-
1 e-
EF
5 e-
5 e-
0.54 e-
d-DOS at EF is zero
No net magnetization
Cu 3d104s1

## Slide 20: RKKY interaction

## Slide 21: RKKY interaction

## Slide 22: Spatially varying fields
RKKY interaction (Ruderman-Kittel-Kasuya-Yosida)
F(2kfr)
kfr/π

## Slide 23: Ferromagnetic magnons
Magnetic energy (Heisenberg)
In groundstate (classical S)
First excited state ?
No !
share spin-flip
with all  Magnons