## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Previously
Crystal = Lattice + Basis
Primitive unit cells
Symmetry: Translations, Rotations
Classification -> Bravais lattices

## Slide 3: Today
Binding Attractive and repulsive potentials
Lattice sums, cohesive energy, equilibrium structure
Reciprocal space
Diffraction

## Slide 4: BINDING
Kittel Ch.3

## Slide 5: Water
Freezing point
Kinetic energy vs Potential energy
Density-density correlations
1st
2nd
3rd
G(R)
R

## Slide 6
Kinetic energy:
“Particle in a box”:
~ 4 eV (45.000 K)
Length scale atoms, orbitals, interatomic: r ~ 1 Å
Potential energy:
Coulomb
~ 14 eV (160.000 K)
Ionic: Coulomb interaction
Metals: e- - delocalization

## Slide 7: Cohesive energy
van der Waals: Induced dipole moments Heitler-London: Pauli repulsion Lennard-Jones:
Coulomb:
Covalent: Homopolar bond
Metals: Kinetic energy

## Slide 8: Lennard-Jones potential
U/4e
s/R
0
1
2
3
0
-0.5
0.5

## Slide 9: Molecular Hydrogen
General form wavefunction
Pauli exclusion principle: Heitler-London approach
Correlations: no two electrons on the same site

## Slide 10
U (Ry)
R (a0)
0
-0.2
2
0
4
0.2
6
Triplet - anti-bonding
Singlet - bonding
Classical

## Slide 11: Lattice summations
(FCC: 12.13; 14.45)
No net forces:
Cohesive energy:
Lennard-Jones:

## Slide 12: Linear ionic crystal
+
-
+
+
-
-
+
-
Madelung constant

## Slide 13
+
-
+
+
-
-
+
-
R
pij
1
3
2
U
R
Repulsive
Coulomb
Total

## Slide 14: DIFFRACTION & RECIPROCAL SPACE
(Kittel Ch. 2)

## Slide 15: Crystal Structure
Reciprocal lattice
Symmetry, Extinction conditions
Primitive reciprocal lattice vectors
Wigner Seitz cell, Brillouin zones
Examples: SC, BCC, FCC lattices
Diffraction intensity
Atomic form factor
Structure factor
Diffraction pattern
Lattice
Basis
+
Diffraction
Lattice vibrations
Electronic properties
Bloch functions
Fourier Transform
periodic structure

## Slide 16: Diffraction: Bragg law
d
q
Constructive interference:

## Slide 17: Diffractometer

## Slide 18: X-rays, electrons, neutrons
0.1
1
10
10-3
101
105
E (eV)
l (Å)
g
e-
n

## Slide 19: Beryl ( Be3Al2(SiO3)6 )

## Slide 20: Molybdenum oxide MoO3
Orthorhombic MoO3

## Slide 21: Reciprocal Space
Periodic plane waves in periodic structures
Set of directions in the real lattice
Set of allowed Fourier components in FT from structure

## Slide 22: Reciprocal lattice
ai·bj=2pdij
b1, b2, b3 are primitive lattice vectors of an abstract lattice, conjugate to the lattice in direct space. They span a Bravais lattice.
bj not easily scalable to ai and not parallel to them either
Reciprocal of reciprocal is real lattice again
dimension [bi] = m-1

## Slide 23: Reciprocal lattice of SC
V=a3
V=(2p/a)3

## Slide 24: Reciprocal lattice of FCC
This is BCC !
V=a3/4

## Slide 25: Fourier analysis
Translational invariance:
FT
Back

## Slide 26: Fourier analysis
FT
Structure factor:
Direct space periodicity:

## Slide 27: Crystal Structure
Reciprocal lattice
Diffraction intensity
Structure factor
Atomic form factor
Diffraction pattern
Lattice
Basis
+
Fourier Transform
periodic structure

## Slide 28: Atomic form factor
Structure factor:
e.g.
Atomic form factor:

## Slide 29: Diffraction conditions
Theorem: The set of reciprocal vectors
determines the possible x-ray reflections
Scattering from k to k’ is proportional to n(r)
Periodicity n(r) =>
Scattering amplitude:
Laue condition
Ewald construction
Brillouin construction

## Slide 30: CsCl, exponential charge distributions
Atomic form factors:

## Slide 31: CsCl, diffraction conditions
Structure factor:
Simple cubic lattice, Bragg condition:
h+k+l even
h+k+l odd

## Slide 32: Case I: fA >> fB
S(h,k,l)
0
(100)
(110)
(111)
(200)
(210)
0

## Slide 33: Case II: fA = fB
S(h,k,l)
0
(100)
(110)
(111)
(200)
(210)
0

## Slide 34: Pseudo-bcc
Diffraction for
with h + k + l even (fA = fB) : 'pseudo-bcc‘
S.C.
B.C.C.