## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Previously
Free electron model
Density of states, Fermi-Dirac distribution
Pressure, Bulk modulus, Heat capacity, Thermal mass

## Slide 3: Today
Transport
Failures of the free electron model
Incorporating periodicity

## Slide 4: Electrical conductivity
k
k’
dk
F
2nd Newton: or
Relaxation time t: dk 0
e-p,e-e scattering (appendix J, Ch. 10)
Impurity scattering
Equation of motion:

## Slide 5: Electrical conductivity
ky
kx
E

## Slide 6: Electrical conductivity
ky
kx
E

## Slide 7: Ohm’s law
F = qE
Current density
Ohm’s law
Very pure metals, low T:
s -1
T
Notes: Scattering phonons, impurities. Matthiessen’s rule; low T temperature dependence (#phonons)
Residual resistance ratio;

## Slide 8
Resistance of potassium
at 20 K for two different
samples.
Residual resistance ration RRR
An impurity causes a residual
resistance of:

## Slide 9
Temperature dependence of the electric resistance
Very low temperatures
Phonon T5/ D5
Umklapp-processes are not possible
for T<2K in the case of K
(2) Low temperatures
Umklapp-processes become possible
<n>  e-U/T characteristic Umklapp-temperature
Potassium: U=23K; D=91K
(3) High temperatures
<n>  T  Phonon T
(4) Very high temperatures
saturation as the phonon scattering cannot lead to mean free path-lengths
shorter than the lattice constant (Ioffe rule)

## Slide 10
The resistance roughly scales with the Debye temperature !

## Slide 11
Transition from T5 to T behavior !

## Slide 12
Matthiessen rule: alloys vertical displacement of (T) curves

## Slide 13: 1D conduction