## Slide 1: Condensed Matter Physics I
Prof. Dr. Ir. Paul H.M. van Loosdrecht
II Physikalisches Institut, Room 312
E-mail: pvl@ph2.uni-koeln.de
Website: http:/www.loosdrecht.net/

## Slide 2: Previously
Free electron model
Density of states, Fermi-Dirac distribution
Pressure, Bulk modulus, Heat capacity, Thermal mass
Charge conductivity
Classical Hall effect
Electronic thermal transport, Wiedemann-Franz
Failures of free e- model
Incorporation periodic potential, Bloch states, gaps

## Slide 3: Today

## Slide 4: Band structure: Approaches
Empty lattice (only periodicity)
Perturbation theory (nearly free electrons, weak potential)
Tight binding method (LCAO)
Exact models (Kronig-Penney model, see for instance Kittel)
‘advanced’ methods: see for instance ashcroft and mermin, chapter 11

## Slide 5: Diamond band structure

## Slide 6: Sr2RuO4

## Slide 7: Photoemission
Gold, U. Johansson, R. Nyholm

## Slide 8: Photoemission

## Slide 9: Photoemission

## Slide 10: Photoemission

## Slide 11: Band Structure
Continued

## Slide 12: Bloch theorem
The eigenstates of a periodic one-electron Hamiltonian can be chosen to have the form of
a plane wave times a function with the periodicity
of the Hamiltonian
Bloch Theorem

## Slide 13: Remarks on Blochfunctions
Quantum number k: Crystal momentum
k may be confined to the 1st BZ (Reduced BZ)
Band index n Born-von Karman
Band structure

## Slide 14: Band structure: Approaches
Last time
  Empty lattice (only periodicity)
  Perturbation theory (nearly free electrons, weak potential)
Today
  Tight binding method (LCAO)
Other methods
  Exact models (Kronig-Penney model, see book)
  ‘advanced’ methods: Ashcroft & Mermin chapter 11

## Slide 15: Tight binding approach
1
2
3
4
5
6
7
8
9
r/a0
E
H=Hat
H=Hat + V(r)

## Slide 16: Tight binding
Atomic orbitals j(r) : Hat j(r) = Eat j(r)
Solid state: H = Hat + V(r)
1st order correction to energy: diagonal elements

## Slide 17: Tight binding
Only nearest neighbours:
Self
N.N.

## Slide 18: Tight binding
S.C.: n.n. at (±a, 0, 0); (0, ±a, 0); (0, 0, ±a)
e(k) = -a - 2g [ cos(kxa) + cos(kya) + cos(kza) ]
(kx,0,0)
4g in the (100) dir.
-a
E

## Slide 19: Tight binding
TB method: Insulators and core electrons and d-electrons in transition metals (e.g. Cu, V, Ti etc.).
Nearly free electron model: conduction electrons, s or p, alkali (e.g. Na, K, etc.)

## Slide 20: Reduced Brillouin zone
p/a
-p/a
3p/a
-3p/a
k
E

## Slide 21: Extended zone scheme
p/a
-p/a
3p/a
-3p/a
k
E
2G
-2G
G
-G

## Slide 22: Reduced zone scheme
p/a
-p/a
k
E

## Slide 23: Periodic zone scheme
p/a
-p/a
3p/a
-3p/a
k
E

## Slide 24: Bandstructure
Why are not all solids metals
Why is diamond an insulator
Why is copper a metal
Why does the conductivity of Si increase upon heating
10-20
10-16
10-12
10-8
10-4
100
104
108
Fused silica
Diamond
glass
Silicon
Iron
Copper
Semicond’s
Metals
Insulators
Conductivity (W-1cm-1)
Germanium

## Slide 25: Conductivity
p/a
-p/a
k
E
Metal
Insulator
p-Doped
Semi-
Conductor
n-Doped
Semi-
Conductor
C
V

## Slide 26: Diamond and Germanium
Diamond (Eg=5.5 eV)
Germanium (Eg=0.7 eV)

## Slide 27: Bandfilling & overlap
E
E
E
DOS
DOS
DOS
VO2
Partially filled d-bands
TiS2
Overlapping bands
TiO2
Empty d-bands
Ti 3d (eg)
Ti 3d (tg)
Ti 3d (eg)
Ti 3d (tg)
V 3d (eg)
V 3d (tg)
O 2p
O 2p
S 3p
Ti: [Ar]3d24s2
V: [Ar]3d34s2

## Slide 28: Band gap in some materials
Eg(eV)
Diamond I 5.4
Si I 1.17
Ge I 0.74
GaAs d 1.52
GaSb d 0.81
Te d 0.33
ZnO 3.44
Cu2O d 2.17
CdTe d 1.6
TiO2 3.03
Conduction
Valence
Forbidden
Eg
Direct & indirect
Optical absorption